TEST DATA REPORT REQUIREMENTS FOR VINYL MATERIALS

Checklist for HSB Submissions

The minimum information required by PPI's HSB to develop recommendations of HDB/PBD/SDB/MRS for specific thermoplastic pipe and fitting materials is summarized in the following submission checklist for Vinyl materials.  The HSB may require additional information for certain cases.

Complete all sections. Send to the HSB Chairman, along with the signed certification below:

CERTIFICATION TO ACCOMPANY SUBMISSIONS TO THE HSB

I do hereby certify that the data and other information included with this submission are truthful and accurate; that the data are derived from testing actually performed on the samples identified in the submission by the laboratory listed below:

Name of Laboratory:

Address:

Technician:

Date of Testing:

And that the data do not, in any way, misrepresent the performance or other characteristics of the material covered by the submission; and that this submission does not omit any data or information known to my company (including that derived from any testing summarized in this submission) which would be material to an HSB decision on the action requested.

Signed:

Authorized Representative

Printed Name:

Title:

Company:

Date:

Consult PPI TR-3 for Definitions, etc.	Date:

| 1 - Owner of Proposed PPI Listing |
| --- |
|  | Manufacturer: |  |  |
|  | Address: |  |  |
|  | Phone: | ( ) | Fax: | ( ) |  |
|  | Contact: |  |  |

| 2 - Data Submission: |
| --- |
|  | Compound Designation: |  |  |
|  | Submission is a: | New PVC Formulation (see 6.1.1) |  |
|  |  | New Compound (See 6.1.3), for: | PPI Range Formulation |  |
|  |  | (check one of the following:) | Private Formulation |  |
|  |  | PVC Resin (6.1.2) | Other component not complying |  |
|  |  | Process Aid | to the guidelines of PPI TR-3: |  |
|  |  | Heat Stabilizer |  |  |  |
|  |  | Commercial Designation | Specify |  |
|  |  | of the new Component: |  |  |
|  |  | (Attach Physical Property Data Sheet) |  |  |
|  | Special Case (Attached an explanation of why it should be considered) |  |

| 3 - Compound Mixing: |
| --- |
|  | Equipment: | High Intensity Mixer | Low Intensity Cooler |  |
|  |  | or | or |  |
|  |  | Describe Other | Describe Other |  |
|  | Procedure: | Double Batching | or | Single Batching |  |
|  | Description: |  |  |
|  | (Describe the procedure |  |  |
|  | followed in preparing |  |  |
|  | the compound. See Note |  |  |
|  | 7 of TR-3) |  |  |

Consult PPI TR-3 for Definitions, etc.	Date:

| 4 - Fabrication Process: |
| --- |
|  | 4.1 - Extrusion: |  |  |
|  |  | Laboratory Equipment and Conditions |  |
|  | Extrusion was done on: | or |  |  |
|  |  | Production Equipment and Conditions |  |
|  | 4.1 - Molding: | Type of Mold | Side Gate | or | End Gate |
|  | Specimen Dimensions, in or mm (Indicate Units): |  |
|  | Outside Diameter: |  | Wall Thickness: | / | Length: |  |  |
|  |  | Average |  | Minimum | Average |  | Average |  |

| 5 - Resin and/or Compound Properties: |
| --- |
|  | 5.1 - Resin Properties: |  |
|  | (Only required if PVC Resin box was checked in Section 2) | Lot 1 |  | Lot 2 |  | Lot 3 |  |  |
|  |  | ( (if required) ( |  |  |
|  | Inherent Viscosity | ASTM D1243 |  |  |  |  |  | (0.88 - 0.96) |  |
|  | Heat Loss (water) % by wt. | 1 hr @ 2210F (1050C) |  |  |  |  |  | (0.5 max.) |  |
|  | Apparent Bulk Density, g/cc | ASTM D1895 |  |  |  |  |  | (0.46 - 0.62) |  |
|  | Compacted Bulk density, g/cc | ASTM D1895 (Method C) |  |  |  |  |  | (0.54 - 0.72) |  |
|  | RVCM | ASTM D3749 |  |  |  |  |  | (10 ppm max.) |  |
|  | 5.1 - Compound Properties: |  |
|  | Cell Classification per ASTM D1784: |  |  |
|  | Actual Values (indicate units): |  |
|  | Base Resin |  | PVC |  |
|  | Izod Impact Strength, ft-lb/in or J/m | ASTM D256 Method A |  |  |
|  | Tensile strength, psi or MPa | ASTM D638 |  |  |
|  | Modulus of elasticity, psi or MPa | ASTM D638 |  |  |
|  | Deflection temperature under load, 0F or 0C | ASTM D648 |  |  |
|  | [264 psi (1.82 MPa) load] |  |  |  |

Consult PPI TR-3 for Definitions, etc.	Date:

| 6 - Hydrostatic Stress/Time Requirements |
| --- |
|  | 6.1 - Data Required: |  |
|  | 6.1.1 - New PVC Formulation: | Provisional Listing |  | Standard Listing |  |
|  |  | ( E2 followed by ( E4, E6, etc. every 6 months. |  | E10 on one lot plus ( E2 on two additional lots. |  |
|  | 6.1.2 - New PVC Resin:: | Provisional Listing |  | Standard Listing |  |
|  | (stabilizer and calcium carbonate must be at the maximum of range). | ( E6 followed by ( E8, etc. every 6 months. |  | E10 on one lot plus ( E2 on two additional lots. |  |
|  | 6.1.3 - New Component: | Provisional Listing |  | Standard Listing |  |
|  | (subject component must be at the maximum of range). | ( E6 followed by ( E8, etc. every 6 months. |  | E10 on one lot plus ( E2 on two additional lots. |  |
|  | 6.1.4 - Special Case: |  |  |
|  | (what protocol is proposed?) |  |  |
| 6.2 - Stress/Time Data: |
|  | 6.2.1 - Use the forms in Section 8 to provide the stress, time and failure mode for each lot of pipe that was tested. All data points must be reported even though they may not be considered appropriate for the calculation. The reason for the latter is to be given. |  |
|  | 6.2.2 - Indicate the mode of failure using the following codes: |  |
|  | N - Non-failure point | B - Brittle |  |
|  | S - Shatter | ? - Other, Specify |  |
|  | D - Ductile |  |  |
|  | 6.2.3 - Calculate the 100,000-h LTHS, 50-year intercept, LCL and LCL Ratio and show these results in Section 8. |  |
|  | 6.2.4 - Computer printouts of the data and calculations are acceptable if they provide all the information requested in Section 8 in an easy to read format. |  |

| 7 - Hydrostatic Stress Summary: (Indicate the units) |
| --- |
|  | HDB/PDB/SDB/MRS requested |  | psi or MPa |  |

Consult PPI TR-3 for Definitions, etc.	Date:

| 8 - Actual Stress/Time Data: |
| --- |
|  | Lot # _____________ |  | Lot # _____________ |  |
|  | Size, In: |  |  |  | Size, In: |  |  |  |
|  | SDR # or SCH #: |  |  |  | SDR # or SCH #: |  |  |  |
|  | Stress psi | Time h | Failure Mode (see 6.2.2) |  | Stress psi | Time h | Failure Mode (see 6.2.2) |  |
|  | 100,000 h LTHS: |  | psi or MPa |  | 100,000 h LTHS: |  | psi or MPa |  |
|  | 50 Year intercept: |  | psi or MPa |  | 50 Year intercept: |  | psi or MPa |  |
|  | LCL: |  | psi or MPa |  | LCL: |  | psi or MPa |  |
|  | LCL Ratio: |  | % |  | LCL Ratio: |  | % |  |
|  | Temperature: |  | 0C or 0F |  | Temperature: |  | 0C or 0F |  |
|  |  | Environment: |  |  | Environment: |  |
|  | Inside Pipe: |  |  |  | Inside Pipe: |  |  |  |
|  |  | Outside Pipe: |  |  |  | Outside Pipe: |  |  |  |
|  |  | 2 | 4 | 6 | 8 | 10 |  |  |  |  | 2 | 4 | 6 | 8 | 10 |  |  |  |
|  | E Level: |  |  |  |  |  |  |  |  | E Level: |  |  |  |  |  |  |  |