TEST DATA REPORT REQUIREMENTS FOR NON-PVC MATERIALS

Checklist for HSB Submissions

The minimum information required by PPI's HSB to develop recommendations of HDB/PBD/SDB/MRS for specific thermoplastic pipe and fitting materials is summarized in the following submission checklist for non-PVC materials.  The HSB may require additional information for certain cases.

Complete all sections. Send to the HSB Chairman, along with the signed certification below:

CERTIFICATION TO ACCOMPANY SUBMISSIONS TO THE HSB

I do hereby certify that the data and other information included with this submission are truthful and accurate; that the data are derived from testing actually performed on the samples identified in the submission by the laboratory listed below:

Name of Laboratory:

Address:

Technician:

Date of Testing:

And that the data do not, in any way, misrepresent the performance or other characteristics of the material covered by the submission; and that this submission does not omit any data or information known to my company (including that derived from any testing summarized in this submission) which would be material to an HSB decision on the action requested.

Signed:

Authorized Representative

Printed Name:

Title:

Company:

Date:

| 1 - Owner of Proposed PPI Listing |
| --- |
|  | Manufacturer: |  |  |
|  | Address: |  |  |
|  | Phone: | ( ) | Fax: | ( ) |  |
|  | Contact: |  |  |

Consult PPI TR-3 for Definitions, etc.	Date:

| 2 - Data Submission: |
| --- |
|  | Compound Designation: |  |  |
|  | Compound is Intended for | Extrusion Only |  |
|  |  | Molding Only |  |
|  |  | Either Extrusion or Molding |  |
|  | Data Submission is for a: | New Formulation |  |
|  |  | Modified Formulation |  |
|  |  | Base, (or Parent), Formulation is: |  |  |
|  | Description of Modification |

| 3 - Type of Request: |
| --- |
|  | Routine Request: | The data and other information herewith presented are in full compliance with PPI TR-3 requirements for the requested level, (E2, E4, E6, etc.) of PPI listing. |  |
|  | Special Case: | Some of the information, as follows, is not in full compliance with the TR-3 requirements: |  |
|  |  | Notwithstanding this, it is believed that the data presented are sufficient for granting the request listing based on the following reasons: |  |
|  |  | (Note: Special Cases are referred to the HSB for adjudication) |  |

Consult PPI TR-3 for Definitions, etc.	Date:

| 4 - Requested Action: |
| --- |
|  | Based on this data submission the following action is requested: |  |
|  |  | A listing of the subject formulation (see Note) for the listing level, (Standard, E2, |  |
|  |  | E4, E6, etc.) of |  | , |  |
|  |  | for a recommended HDB/PDB/SDB/MRS of |  | psi, |  |
|  |  | for a temperature of |  | 0F (or 0C, specify), and |  |
|  |  | external environment of |  | . |
|  |  | Acceptance of the subject formulation as equivalent to the base formulation. It is requested that this equivalent formulation be listed under: |  |
|  |  | Its own identification, which is: | , |  |
|  |  | or |  |  |
|  |  | The Base formulation. |  |  |
|  | (Note: Consult PPI TR-3, Parts A & B for listing grades, conditions and requirements) |

| 5 - Other Data or Listings: |
| --- |
|  | Does this material have a PPI listing at other temperatures or conditions? | No |  |
|  |  | Yes (Provide the details) |  |
|  | Are there stress-rupture data available for other temperatures? | No |  |
|  |  | Yes - Have been previously submitted |  |
|  |  | (List the temperatures in 0C or 0F) |  |
|  |  | Yes - Are now being submitted via separate data submissions |  |
|  |  | (List the temperatures in 0C or 0F) |  |

Consult PPI TR-3 for Definitions, etc.	Date:

| 6 - Pipe or Fitting Material Designation and Classification: |
| --- |
|  | ASTM Standard: |  |  |
|  | Cell Classification or Material Identification (all cell class values must be listed). |  |  |
|  | Actual Values (indicate the units): |  |
|  | Physical Property | Test Method | Average Value, or Range |  |
|  | Density, g/cc | ASTM D 1505 |  |  |
|  | Melt Index, g/10 min. | ASTM D 1238 |  |  |
|  | Tensile strength, psi or MPa | ASTM D638 |  |  |
|  | Flexural Modulus, psi or MPa | ASTM D790 |  |  |
|  | Stress Crack Resistance, hrs. | ASTM F 1473 |  |  |
|  | Deflection temperature under load 0F or 0C | ASTM D648 |  |  |
|  | [264 psi (1.82 MPa) load] |  |  |  |
|  | Others: |  |  |  |  |  |

| 7 - Compound Mixing: |
| --- |
|  | Material is: | Pre-Compounded | or | Blended In-Plant |

| 8 - Hydrostatic Stress/Time Data: |
| --- |
| 8.1 - Use the form in Section 10 to provide the stress, time and failure mode for each lot of pipe that was tested (make copies if necessary). All data points must be reported even though they may not be considered appropriate for the calculation. The reason for the latter is to be given. |
| 8.2 - Indicate the Mode of Failure in Section 10, using the following codes: |
|  | N - Non-failure point | B - Brittle |
|  | S - Shatter | ? - Other, Specify |
|  | D - Ductile |  |

Consult PPI TR-3 for Definitions, etc.	Date:

| 8 - Hydrostatic Stress/Time Data (cont’d): |
| --- |
| 8.3 - Is Creep the controlling factor? |
| (See Paragraph 5.3, “Circumferential Expansion”, of ASTM D2837 for details on data requirements for evaluating creep as a potential limiting factor. Based on historical data, PPI’s HSB recognizes the following materials as having long term strengths which are not limited by the ASTM D2837 creep criterion: PVC, medium and high density PE, CPVC, PA & PB.) |
|  | No Present the basis for this conclusion if the material is other than those listed above. |  |
|  | Yes Present the circumferential expansion data summary and resultant calculations on a separate data sheet. |  |
| 8.4 - Calculate the 100,000-h LTHS, 50-year intercept, LCL and LCL Ratio and show these results in Section 10. |  |
| 8.5 - Computer printouts of the data and calculations are acceptable if they provide the information requested in Section 10 in an easy to read format. |  |
| 8.6 - Polyethylene materials, which are to be listed with an HDB at 73(F and at higher temperatures, must also undergo supplemental validation of the long-term hydrostatic strength in accordance with Clause 5.6 of ASTM D2837, or Part F.4 of TR-3. |  |
| Remember to submit these validation data on a separate data sheet. |  |
| 8.7 - For crosslinked polyethylene (PEX) pipe data, what is the measured level of cross-linking for specimens tested? __________________ |
| What is the measurement method? ___________________________________________ |
| The listed HDB/MRS for this PEX pipe will be based on this minimum crosslink level. |
| 9 - Hydrostatic Stress Summary (indicate the units) |
|  | HDB/PDB/SDB/MRS requested: |  | psi or MPa |

Consult PPI TR-3 for Definitions, etc.	Date:

| 10 - Data Submission for Lot #_________: |
| --- |
|  | 10.1 - Actual Stress/Time Data |  | 10.2 - Fabrication Process |  |
|  | Average Outside diameter, in: (approximate values) |  |  |  | 10.2.1 - Extrusion: |  |
|  | Minimum Wall Thickness, in: |  |  |  | Extrusion was done on: |  |
|  |  |  |  |  | Laboratory Equipment and Conditions |  |
|  | Stress psi | Time h | Failure Mode (see 8.2) |  | or Production Equipment and Conditions |  |
|  |  |  |  |  |  |  |  |  |  |  | 10.2.2 - Molding: |  |
|  |  |  |  |  |  |  |  |  |  |  | Type of Mold: |  |
|  |  |  |  |  |  |  |  |  |  |  | Side Gated |  |
|  |  |  |  |  |  |  |  |  |  |  | or |  |
|  |  |  |  |  |  |  |  |  |  |  | End Gated |  |
|  |  |  |  |  |  |  |  |  |  |  | (indicate the units) |  |
|  |  |  |  |  |  |  |  |  |  |  | Outside Diameter: |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Average |  |  |
|  |  |  |  |  |  |  |  |  |  |  | Wall Thickness; | / |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Minimum | Average |  |  |
|  |  |  |  |  |  |  |  |  |  |  | Length: |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Average |  |  |
|  |  |  |  |  |  |  |  |  |  |  | 10.3 - Hydrostatic Properties |  |
|  |  |  |  |  |  |  |  |  |  |  | 100,000 h LTHS: |  | psi or MPa |  |
|  |  |  |  |  |  |  |  |  |  |  | 50 year intercept: |  | psi or MPa |  |
|  |  |  |  |  |  |  |  |  |  |  | LCL: |  | psi or MPa |  |
|  |  |  |  |  |  |  |  |  |  |  | LCL Ratio: |  | % |  |
|  |  |  |  |  |  |  |  |  |  |  | Temperature: |  | 0C or 0F |  |
|  |  |  |  |  |  |  |  |  |  |  | Environment: |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  | Inside Pipe: |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  | Outside Pipe: |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | 2 | 4 | 6 | 8 | 10 |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  | E Level: |  |  |  |  |  |  |  |